## Slide 1
Rare-earth doped
Topological Insulators
4. September, 2018
Myung-Hwa Jung
Department of Physics
Sogang University, Seoul, Korea
Jinsu Kim

## Slide 2: Contents
3D topological insulators (TIs)
Nonmagnetic doping effect
Magnetic doping effect
Rare-earth doped TIs  Antiferromagnetic
Gd-doped Bi2Se3
Gd-doped Bi2Te3
 Possible Weyl semimetal
(Magnetic dopants)
 Gd doping effect
 Vacuum annealing effect
 Tuning effect of EF

## Slide 3
Periodic table
3D Topological insulators (TIs)
A2B3 (A = Sb or Bi & B = Se or Te)
: Sb2Se3, Sb2Te3, Bi2Se3, Bi2Te3
Bi : 6s26p3  Bi3+ : 6s26p0 (or Bi3- : 6s26p6)
Se : 4s24p4  Se2- : 4s24p6
ex) Bi2Se3
: Insulator

## Slide 4: Fermi level issue
k
E
Dirac point
EF
Bulk electron is measured…
(n3D~1019/cm3 vs. n2D~1012/cm2)
EF
 Exotic topological surface properties  EF at the Dirac point
But, difficult to locate the Fermi level at the Dirac point
difficult to distinguish the surface state from the bulk band
BCB
BVB
SS
Δ
ARPES

## Slide 5: EF tuning by annealing (Bi2Te3+)
kx (Å-1)
EB (eV)
Fine tuning of Bi2Te3+ (by Te annealing)

EF
S1
S2
S3
S4
BiTe
(p-type)
TeBi
(n-type)
Antisite defects

## Slide 6
Non-metallic
x = 0.025
x > 0.01
x = 0
PRL 103, 246601 (2009)
Fine tuning of EF by doping (Bi2-xCaxSe3)
Metallic
Metallic
Se vacancies
(n-type)
Ca2+ instead of Bi3+  (p-type)

## Slide 7: Magnetic doping (Bi2-xTrxSe3)
Gap opening (magnetic Fe)
FM  Spin-related applications
Quantum phenomena
Science 329, 5992 (2010)
Science 340, 167 (2013)
QAHE
Crx(Bi,Sb)2-xTe3
FM
EF
No gap opening (nonmagnetic Tl)
nonmagnetic
magnetic

## Slide 8
Transition metals (Tr2+)
Tr : 4s23dn  Tr2+ : 4s03dn
Periodic table
Bi3+
Bi2-xTrxTe3: Trivial topological insulator
Tr2+ ( 4s04p03dn )  Doping of charge carriers (hole doping)
 Tuning magnetism (only FM ordering)

## Slide 9
Periodic table
Bi3+
Bi2-xLnxTe3: Another type of magnetic TIs?
Ln3+ ( 5s25p64fn )  No doping of charge carriers?
 Tuning only magnetism (AFM ordering?)
Rare-earth metals (Ln3+)
Gd : 6s24f8  Gd3+ : 6s04f7 (~7μB)

## Slide 10: Antiferromagnetism in GdxBi2-xSe3
 Weak antiferromagnetic signal at x  0.3
x | Type | n ( cm-3 ) | θ P ( K ) | TN ( K )
0.15 | n |  | -0.70 | -
0.20 | n |  | -1.85 | -
0.30 | n |  | -6.83 | 6.2
0.40 | n |  | -7.98 | 7.0
PM
AFM

## Slide 11: Competing TSS with AFM in GdxBi2-xSe3
 |  | (Berry phase factor)
 | 1/2 |  2D surface state
 | 0 |  3D bulk band
1/2
Landau level fan diagram

## Slide 12: Gap opening in GdxBi2-xSe3
Bi0.85Gd0.14Se3
 ~ 60 meV
No gap
Gap
AFM  TRS breaking
 Gap opening

## Slide 13: Phase transition in GdxBi2-xTe3
x < 0.09: PM (weak FM)  x > 0.09, AFM
= 12 K

## Slide 14: 2D Fermi surface at x = 0.09
x < 0.09: PM (weak FM)  x > 0.09, AFM
At x = 0.09 (MCP),
= 1/2 for B//c
 2D TSS
x = 0.09
1/2

## Slide 15: Band structure of GdxBi2-xTe3
0.208Å-1
, x=0
NM
PM
AFM

## Slide 16: Gap scale by magnetic dopant
Gd 15%
cf) Bi0.86Gd0.14Se3
 ~ 60 meV
Bi0.85Gd0.15Te3
 ~ 60 meV

## Slide 17: Gap scale by magnetic dopant
Gd3+ ~ 7B
Fe2+ ~ 4B
Gd 15%
24%
Science 329, 5992 (2010)
Our results
Bi0.85Gd0.15Te3
 ~ 60 meV
Bi0.76Fe0.24Te3
 ~ 44 meV

## Slide 18: Annealing effect in GdxBi2-xTe3
: sensitive to surface
Gd peak increases with x
Annealed at 250oC for 2 h
under UHV (1 x 10-10 Torr)
After annealing,
Gd peak ↑
 more populated Gd
Before annealing,
Fitted only with bound Bi
After annealing,
Bound Bi ↓ + Unbound Bi
 Bi out-diffusion
 metallic Bi at surface
Near edge x-ray absorption fine structure (NEXAFS) & XPS
Annealed
As-grown

## Slide 19: Restored TSS after annealing
Before annealing,
( x = 0.15 )
TN = 11.5 K
MR = 360%
β = 0
After annealing,
TN disappears
MR = 1400%
β = 1/2
Two-band Hall
 Restored TSS
C-W fit
 x = 0.10 (MCP)

## Slide 20: Gap closing after annealing
Bi2Te3
Gd0.15Bi1.85Te3
As-grown
Annealed
Pristine
No gap
Gap opening
Gap closing
(NM)
(AFM)
(PM)

## Slide 21: Microscopic analysis of annealing effect
Before
After
After
Pristine
A  TeBi1
B  TeBi2
C  VBi2
Gd doping
  GdBi2Bii
  GdBi1
After annealing
 disappears.
 increases.
 appears.
 BiTe1
α
β
γ
Quintuple
layer
of Bi2Te3

## Slide 22: Schematic picture upon annealing
Evaporation of top surface Te
 VTe1 (volatile Te)
Migration of adjacent Bi
 BiTe1VBi1 pairs
1
GdBi2
Isolated BiTe1   defect Liberation of VBi1
: Occupied by out-diffused Gd
 GdBi1 ( defect), GdBi2 ( defect)
: increment : removal



Restored TSS

## Slide 23: Tuning effect in GdxBi2-xTe3-ySey (y=0.2)
TN = 9.2 K
LMR
cf) y = 0 ; TN = 9.2 K, p = 29.41018 cm-3
LMR
TMR
LMR
y =0
EF
y = 0.2 | Carrier type | n (cm-3) |  (cm2/Vs)
2 K | p | 5.22  1018 | 7120
300 K | p | 9.93  1018 | 178
(x = 0.1)

## Slide 24: Tuning effect in GdxBi2-xTe3-ySey (y=0.6)
y = 0.6 | Carrier type | n (cm-3) |  (cm2/Vs)
2 K | n | 0.58  1018 | 211
300 K | p | 7.70  1018 | 89
TN = 9.1 K
LMR
LMR
TMR
y =0.2
y =0
y =0.6
EF
cf) y = 0.2 ; TN = 9.2 K, p = 5.221018 cm-3
(x = 0.1)

## Slide 25: Tuning effect in GdxBi2-xTe3-ySey (y=1.5)
y = 1.5 | Carrier type | n (cm-3) |  (cm2/Vs)
2 K | n | 14.1  1018 | 894
300 K | n | 14.5  1018 | 59
TN = 9.0 K
LMR
LMR
TMR
y =0.2
y =0
y =0.6
LMR
TMR
EF
y =1.5
cf) y = 0.6 ; TN = 9.1 K, n = 0.581018 cm-3
(x = 0.1)

## Slide 26: Summary for tuning effect by Se
y | T (K) | ρ (mΩcm) | Carrier type | n (1018cm-3) | μ (cm2/Vs)
1.5 | 2 K | 6.6 | n | 14.1 | 894
 | 300 K | 7.3 |  | 14.5 | 59.4
1.0 | 3 K | 42 | n | 5.36 | 27.5
 | 300 K | 17 |  | 3.31 | 111
0.7 | 2 K | 3800 | n | 0.42 | 3.91
 | 300 K | 25 | p | 5.57 | 45.0
0.6 | 2 K | 57 | n | 0.58 | 211
 | 300 K | 9.1 | p | 7.70 | 88.9
0.5 | 3 K | 7.8 | p | 0.75 | 1060
 | 300 K | 1.0 |  | 4.53 | 136
0.2 | 2 K | 0.2 | p | 5.22 | 7120
 | 300 K | 3.5 |  | 9.93 | 178
0.1 | 2 K | 0.06 | p | 13.3 | 7850
 | 300 K | 1.3 |  | 22.1 | 215
TN = 9.0 ~ 9.2K
n-type
p-type
Crossover point y ~ 0.7

## Slide 27: Evolution of electrical transport
y = 0.1
y = 0.2
y = 0.6
y = 0.7
y = 1.0
y = 1.5
n-type
p-type
Crossover point y ~ 0.7

## Slide 28
ZrTe5, Na3Bi, Cd3As2, Bi1-xSbx,
Y2Ir2O7, HgCr2Se4, Hg1-x-yCdxMnyTe
Time reversal symmetry breaking
TaAs, NbAs, NbP, TaP
Inversion symmetry breaking
Possible Weyl state
  ● Gd (antiferromagnetic ordering)
  : acts as effective magnetic field
   Zeeman splitting
   Reduction of bulk band gap
  ● Se (n-type carrier doping)
  : tunes the Fermi level
   Weyl point at EF
GdxBi2-xTe3-xSey
 Negative LMR
WAL
E·B term  Charge pumping

## Slide 29
ZrTe5, Na3Bi, Cd3As2, Bi1-xSbx,
Y2Ir2O7, HgCr2Se4, Hg1-x-yCdxMnyTe
Time reversal symmetry breaking
Magnetic field (magnetic order)
TaAs, NbAs, NbP, TaP
Inversion symmetry breaking
New Weyl materials
  ● Gd (antiferromagnetic ordering)
  : acts as effective magnetic field
   Zeeman splitting
   Reduction of bulk band gap
  ● Se (n-type carrier doping)
  : tunes the Fermi level
   Weyl point at EF
GdxBi2-xTe3-xSey
E
x = 0
EF
E
x = x1
EF
E
x = x2
EF
E
x = x3
EF
Zero-gap material
Magnetic dopants
E
x = x3, y = y1
EF
E
x = x3, y = y2
EF
E
x = x3, y = y3
EF
Fermi level tuning
x = x3, y = y2
New Weyl material

## Slide 30: Weyl metal state in GdxBi2-xTe3-ySey
Effective field theory
Renormalization group analysis

## Slide 31: Acknowledgements
Thank you
Extreme Quantum Materials Laboratory (EQML)
http://eqml.sogang.ac.kr/ssmc/
e-mail: mhjung@sogang.ac.kr
TI and Weyl
bulk group
Magnetic thin
film group